3-Part CSI MasterFormat Specification

SECTION 10 2600

WALL AND DOOR PROTECTION

# GENERAL

# SECTION INCLUDES

### Corner Guards

### Crash Rails and Bumper Guards

### Handrails

### Protective Wall covering

# SUBMITTALS

### Comply with requirements of Section 01 33 00 Submittals.

### Product data: Submit manufacturer’s product data.

### Shop drawing: Submit shop drawings showing components, dimensions, anchorage details.

### Samples for selection and verification of product pattern and finish.

# QUALITY ASSURANCE

### Design and Performance Criterial

### Flammability Characteristics: High impact vinyl components.

### Class A Interior wall finish (NFPA 101 Life Safety) when tested in accordance with ASTM E84.

### Flame Spread: 25 or less

### Smoke Developed: 450 or less

### Classification of HB when tested in accordance with ASTM D635.

### Stain Resistance: High impact vinyl components.

### Material to be tested for stain resistance to various chemical reagents in accordance with ASTM D543.

### Bacterial and Fungal Growth: High impact vinyl components.

### Material must not support bacteria or fungal growth when tested in accordance with ASTM G21 and ASTM G22

### Impact Resistance: High impact vinyl components.

### Extruded profiles shall resist damage from impact at apex of 90 degree corner when tested in accordance with applicable sections of ASTM F476.

### Izod impact strength ASTM D256 method A notched, 23.8 ft-lbs/in average with no break.

### Charpy impact strength ASTM D6110 notched, 26.1 ft-lbs/in average with

### Single source responsibility:  Provide all product systems components from a single source.

# DELIVERY, STORAGE AND HANDLING

### Delivery:  Deliver materials to site in manufacturer’s original, unopened containers and packaging with labels clearly indicating manufacturer and material.

### Storage: Store materials indoors in a clean, dry area protected from damage where temperature and humidity remain stable and within 40 degree F (4 degree C) to 100 degree F (38 degree C).  Materials must be stored flat.

### Handling: Protect materials during handling and installation to prevent damage

# PROJECT CONDITIONS

### Environmental conditions:  Do NOT install wall surface protection systems until the installation area is enclosed and weatherproof, and until the ambient temperature within the building is maintained at not less than 70 degree F (21 degree C) for not less than 72 hours prior to installation.

### Installation locations must be enclosed weatherproofed, and climate controlled prior to commencing installation.

# WARRANTY

### Submit supplier’s written warranty against defects in material and workmanship.

# PRODUCTS

# Manufacturer

Babcock-Davis

9300 73rd Avenue North

Brooklyn Park, MN  55428

PH:  888.412.3726

www.BabcockDavis.com

# Products

### Crash Rails and Bumper Guards

#### Vinyl Crash Rails Model BCRV: mounted over continuous aluminum retainer.  Exposed surfaces shall be free of wrinkling, chipping, discoloration, or other imperfections.

##### Cover Material:  high impact vinyl acrylic extrusion locked in place

##### Retainer material:  continuous 6063 T-5 aluminum

##### Sizes: 8 inches (203.2 mm)

#### Mounting Options: [Surface mount 1/2 inch (12.7 mm) cushion] [extended mount 1-3/4 inch (45mm)]

#### Color: to be selected from manufacturer options

# EXECUTION

# EXAMINATION

### Examine the substrates and conditions under which the work is to be performed, and notify the Contractor in writing of conditions detrimental to the proper and timely completion of the work. Do not proceed with the installation until unsatisfactory conditions have been corrected.

# PREPARATION

### Surface preparation:  Prior to installation, clean surface to remove dirt, debris and loose particles.  Perform additional preparation procedures as required per the manufacturer’s instructions.

# INSTALLATION

### Install the work of this section in strict accordance with manufacture’s written instructions.

# CLEAN UP COMPLETION

### Upon completion of the work, remove excess materials, debris and rubbish resulting from the installation and leave the area in a clean and orderly condition.

END OF SECTION

Rev 12/17